##### SIKA® CarboDur® COMPOSITE STRENGTHENING SYSTEMS

#### SUMMARY OF PROPERTIES

| Mainly Flexural Strengthening Products (Plates) |
| --- |
| Product name | Elastic modulus | Ultimate tensile strain | Width | Thickness |
|  | Εf (kN/mm2) | εfu (-) | bf (mm) | tf (mm) |
| Carbodur S512 | 165 | 0.0170 | 50 | 1.2 |
| Carbodur S612 | 165 | 0.0170 | 60 | 1.2 |
| Carbodur S812 | 165 | 0.0170 | 80 | 1.2 |
| Carbodur S1012 | 165 | 0.0170 | 100 | 1.2 |
| Carbodur S1212 | 165 | 0.0170 | 120 | 1.2 |
| Carbodur S1512 | 165 | 0.0170 | 150 | 1.2 |
| Carbodur S614 | 165 | 0.0170 | 60 | 1.4 |
| Carbodur S914 | 165 | 0.0170 | 90 | 1.4 |
| Carbodur S1014* | 165 | 0.0170 | 100 | 1.4 |
| Carbodur S1214 | 165 | 0.0170 | 120 | 1.4 |
| Carbodur M514 | 210 | 0.0135 | 50 | 1.4 |
| Carbodur M614 | 210 | 0.0135 | 60 | 1.4 |
| Carbodur M914 | 210 | 0.0135 | 90 | 1.4 |
| Carbodur M1014* | 210 | 0.0135 | 100 | 1.4 |
| Carbodur M1214 | 210 | 0.0135 | 120 | 1.4 |
| Carbodur H514 | 300 | 0.0045 | 50 | 1.4 |
| * No product off the shelf. Please ask for time of delivery. |

| Mainly Shear Strengthening Products (L-shaped Strips) |
| --- |
| Product name | Elastic modulus | Ultimate tensile strain | Width | Thickness |
|  | Ef (kN/mm2) | εfu (-) | bf (mm) | tf (mm) |
| Carboshear 4/20/50 | 120 | 0.019 | 40 | 1.4 |
| Carboshear 4/30/70 | 120 | 0.019 | 40 | 1.4 |
| Carboshear 4/50/100 | 120 | 0.019 | 40 | 1.4 |

| Mainly Shear Strengthening or Confinement Products (Flexible Sheets) |
| --- |
| Product name | Elastic modulus | Ultimate tensile strain | Width | Thickness |
|  | Ef (kN/mm2) | εfu (-) | bf (mm) | tf (mm) |
| SikaWrap Hex-103C | 231 | 0.015 | 600 | 0.34 |
| SikaWrap Hex-160C 0/90 | 230 | 0.015 | 600 | 0.045** |
| SikaWrap Hex-230C | 231 | 0.017 | 300/600 | 0.12 |
| SikaWrap Hex-430G | 70 | 0.031 | 300/600 | 0.17 |
| SikaWrap Hex-100G | 72.4 | 0.037 | 600 | 0.36 |
| ** Per fiber direction. |

# Text boxes

For updated information please consult the homepage:

http://bauchemie.sika.ch/html/export/html/exp_frame.htm